| TDS TECHNICAL DATA SHEET |
| --- |
| VR ® 6305 PLATINUM GOLD |
| Assays |  | Values | Method |
| Content | CAS-No. | CI-No. |  |  |  |
| Synthetic Mica | 12003-38-2 |  | 41 ~ 59 | wt % | VOLOR |
| TiO2 | 13463-67-7 | 77891 | 36 ~ 44 | wt % | VOLOR |
| Fe2O3 | 1309-37-1 | 77491 | 5~ 13 | wt% | VOLOR |
| SnO2 | 18282-10-5 | 77861 | 0~2 | wt% | VOLOR |
| Visual evaluation |  |  |  |  |
| Color |  | pass |  | VOLOR |
| Luster |  | pass |  | VOLOR |
| Density |  | 3.0~3.4 | g /cm3 | ISO 787-10 |
| Bulk density |  | 40~48 | g /100ml | DIN 53466 |
| Particle size | 90 % within the range 10-60μm | pass |  | Laser diffraction |
| PH – value | 10 % aqueous slurry | 6 ~ 10 |  | ISO 787-9 |
| Loss on drying | 105 ℃ | < 0.5 | wt % | ISO 787-2 |
| Oil absorption |  | 50 ~ 90 | g oil/100g power | ISO 787-5 |
| Conductance |  | ≤300 | μs/cm | ISO 787-14 |
| Heavy metals | Pb | ≤10 | ppm | VOLOR |
|  | As | ≤1 | ppm | VOLOR |
|  | Hg | ≤1 | ppm | VOLOR |
|  | Cd | ≤1 | ppm | VOLOR |
|  | Sb | ≤1 | ppm | VOLOR |
|  | Cr | ≤100 | ppm | VOLOR |
|  | Ba | ≤50 | ppm | VOLOR |
|  | Cu | ≤50 | ppm | VOLOR |
|  | Ni | ≤10 | ppm | VOLOR |
| Microorganisms | organisms | <100 | CFU/g | MP-35 |
|  | pathogens | absent | In 1g | MP-35 |
| REMARK: The production complies with the requirements by E171 and E172(commission directive 95/45), FDA(21 CFR73.2496; CFR73.2575;2550 and 73.2299) |
| GUANGDONG VOLOR PEARL PIGMENT CO., LTD. No. 28 Industrial Road, Fuxi Industrial Zone, Sihui City, Guangdong, China. Tel: 0086-758-3851111 Fax: 0086-758-3851599 Home Page: www.weinuochem.com E-mail: weinuo1@weinuochem.com volor@china.com |