|  |  |  |  |  | # TDS # TECHNICAL DATA SHEET |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| VR ® 6574 BLUE CRYSTAL |  |  |  |  |  |  |  |
| Assays |  |  | Values |  |  | Method |  |
| Content | CAS-No. | CI-No. |  |  |  |  |  |
| Synthetic Mica | 12003-38-2 |  | 78~84 | wt % |  |  | VOLOR |
| TiO2 | 13463-67-7 | 77891 | 16~20 | wt % |  |  | VOLOR |
| SnO2 | 18282-10-5 | 77861 | 0~2 | wt% |  |  | VOLOR |
| Visual evaluation |  |  |  |  |  |  |  |
| Color |  |  | pass |  |  |  | VOLOR |
| Luster |  |  | pass |  |  |  | VOLOR |
| Density |  |  | 2.7~3.2 | g /cm3 |  |  | ISO 787-10 |
| Bulk density |  |  | 36~44 | g /100ml |  |  | DIN 53466 |
| Particle size | 90 % within the range 60-320μm |  | pass |  |  |  | Laser diffraction |
| ### PH – value | 10 % aqueous slurry |  | 6 ~ 9 |  |  |  | ISO 787-9 |
| Loss on drying | 105 ℃ |  | < 0.5 | wt % |  |  | ISO 787-2 |
| Oil absorption |  |  | 50 ~ 90 | g oil/100g power |  |  | ISO 787-5 |
| Conductance |  |  | ≤300 | μs/cm |  |  | ISO 787-14 |
| Heavy metals | Pb |  | ≤10 | ppm |  |  | VOLOR |
|  | As |  | ≤1 | ppm |  |  | VOLOR |
|  | Hg |  | ≤1 | ppm |  |  | VOLOR |
|  | Cd |  | ≤1 | ppm |  |  | VOLOR |
|  | Sb |  | ≤1 | ppm |  |  | VOLOR |
|  | Cr |  | ≤100 | ppm |  |  | VOLOR |
|  | Ba |  | ≤50 | ppm |  |  | VOLOR |
|  | Cu |  | ≤50 | ppm |  |  | VOLOR |
|  | Ni |  | ≤10 | ppm |  |  | VOLOR |
| Microorganisms | organisms |  | <100 | CFU/g |  |  | MP-35 |
|  | pathogens |  | absent | In 1g |  |  | MP-35 |
| REMARK: The production complies with the requirements by E171 and E172(commission directive 95/45), FDA(21 CFR73.2496; CFR73.2575;2550 and 73.2299) |  |  |  |  |  |  |  |
| GUANGDONG VOLOR PEARL PIGMENT CO., LTD. No. 28 Industrial Road, Fuxi Industrial Zone, Sihui City, Guangdong, China. Tel: 0086-758-3851111 Fax: 0086-758-3851599 Home Page: www.weinuochem.com E-mail: weinuo1@weinuochem.com volor@china.com |  |  |  |  |  |  |  |